# Tension Plate Processing Procedures

# (03/09/01)

- Fit tension plate to a HV plate and sand/file edges until tension plate fits loosely in HV plate.

- Clean tension plate in ultrasound with isopropyl alcohol

- Weigh tension plate and record in weight sheet.

- Insert capacitor barrel assembly in HV plate

- Insert gas fittings in tension plate

- Mount tension plate on HV plate. Line up capacitor barrel to holes on tension plate

- Seal around capacitor barrel and gas fitting on top surface of tension plate (AY103)

- Apply weight on tension plate if plate bows up too much (that capacitor barrel doesn’t get through the hole).

- Let cure overnight.

- Remove tension plate from HV plate

- Flip tension plate inner side up in the Aluminum glue plate

- Seal around capacitor barrel  and eyelet with (AY103)

- Seal over electronics sockets

- Keep glue 1mm away from edge of tension plate

- Let cure overnight

- Weigh tension plate and record in weight sheet.